## Slide 1: Physics and chemistry of nanostructures
Kick-off meeting Navolchi project
February 3th, 2012
Prof. Zeger Hens
Ghent University
Belgium

## Slide 2: PCN
Inorganic and physical chemistry department
Krijgslaan 281—S3
Prof. Z. Hens
2 Postdocs, 10 PhD students
Part of
Center for Nano- and Biophotonics

## Slide 3: Research activities
A research group on (colloidal) nanomaterials
Physics and chemistry of nanostructures
Colloidal synthesis of nanoparticles
Analysis of surface chemistry
Processing and deposition
Characterization of physical properties
Applications in photonics
chemistry
physics
technology

## Slide 4: Research activities
A research group on (colloidal) nanomaterials
Synthesis development
  II-VI, IV-VI, Pb- and Cd-free quantum dots
Structural characterization
  Elemental analysis / HR-TEM imaging / NMR spectroscopy
Development of processing technology
  Ligand engineering / monolayers and thin films / surface patterning / embedding in thin films / QD based devices
Characterization of physical properties
  QD absorption / photoluminescence (steady state, excitation, time-resolved) / non-linear properties (Kerr-effect, photo-induced absorption, gain)
Application development
  Integrated photonics / photovoltaics / white LEDs

## Slide 5: Role within Navolchi
Optical amplifiers based
on colloidal QDs as gain media

## Slide 6: IR Quantum Dots
Based on Pb chalcogenide nanocrystals
Wavelength size tunable, 800-3000 nm
Highly efficient photoluminescence (up to 100% for PbS)

## Slide 7: IR Quantum Dots
Gain with Pb chalcogenide nanocrystals?
HOMO & LUMO 8-fold degenerate
Population inversion requires > 4 excitons/QD
Bandgap in L point
of Brillouin zone

## Slide 8: IR Quantum Dots
Gain with Pb chalcogenide nanocrystals?
HOMO & LUMO 8-fold degenerate
Population inversion requires > 4 excitons/QD
Problem – Auger recombination limits gain lifetime
Bandgap in L point
of Brillouin zone

## Slide 9: IR Quantum Dots
Possible solutions
Increase level spacing between exciton levels
  Due to intervalley coupling and exchange interaction
Expected to be enhanced in PbS quantum rods

## Slide 10: IR Quantum Dots
Possible solutions
Lift exciton degeneracy via Coulomb interactions in heterostructures
  Possible by using quantum dot heterostructures
0
Degeneracy lifted when

## Slide 11: IR Quantum Dots
Possible solutions
Lift exciton degeneracy via Coulomb interactions in heterostructures
  Possible by using quantum dot heterostructures
0
Degeneracy lifted when
Type 2 band alignment
Interfacial energy barrier

## Slide 12: IR Quantum Dots
Possible solutions
Reduce rate of Auger recombination
  heterostructures with gradual interfaces
  Use rods instead of dots (volume scaling)

## Slide 13: Our approach within Navolchi
Development of PbS rods and PbS/CdS heterostructures

## Slide 14: Status of the work
PbS quantum rods synthesized via cation exchange
CdS
Cu2S
PbS
3.7 nm
28 nm
3.7 nm
28 nm

## Slide 15: Status of the work
Enhanced Stokes shift indicates increased exciton splitting
200 meV vs. 60 meV for PbS dotsat same energy

## Slide 16: Status of the work
PbS/CdS multiple dot-in-rods
  Successive cation exchange steps transform original CdS rod into a PbS/CdS multiple dot-in-rod
  Passivation by CdS enhances PLQY to 45-55%
  Justo et al., submitted to JACS

## Slide 17: Status of the work
PbS/CdS dot-in-rods
CdS
PbS

## Slide 18: Status of the work
PbS/CdS dot-in-rods
QR emission shows two features
  Long wavelength feature corresponds to PbS absorption onset
  Short wavelength feature fades out when exciting below CdS band gap

## Slide 19: Status of the work
PbS/CdS dot-in-rods

## Slide 20: Status of the work
PbS/CdS dot-in-rods

## Slide 21: Problems/needs
Characterization of carrier dynamics/light amplification by newly synthesized heterostructures
  Now: pump/probe measurements via informal collaborations
    Strength: understanding of carrier dynamics crucial for achieving gain
    Weakness: too slow for rapid feedback
  Need: alternative method for rapid screening of promising materials
    Setup under development at UGent
    Is further collaboration on this possible within Navolchi consortium?