## Slide 1
Work Package 5 Presentation
Dries Van Thourhout
IMEC, Belgium

## Slide 2: Outline
WP5 Position in Project
Objectives
Tasks
Milestones and Deliverables
Status of Work
Summary and Outlook

## Slide 3: WP3 Position in Project
Contributors:

## Slide 4: Objectives
Overall Objective :
Specific Objectives:
  Coupling light between silicon backbone and plasmonic devices
  Beam Shaping grating couplers to direct light between chips
  Compact filters for noise suppression
  Specify and implement Dual Die Communication Module (DDCM)
Design and implement optical and electrical interfaces for plasmonic interconnect

## Slide 5: Tasks
 | Names of the Tasks | Time Period [months]
Task 5.1 | Modeling and fabrication of coupling Si waveguide to plasmonic waveguide | 1 – 15
Task 5.2 | Design and fabrication of Si beamshaper | 1 – 30
Task 5.3 | Design and fabrication of passive ultra-compact components as filters | 1 – 15
Task 5.4 | Signal generation module design | 4 – 12
Task 5.5 | Signal Generation Module implementation via FPGA | 13 – 24

## Slide 6: Milestones
 | Names of the Milestones | Month | Partner
MS25 | Decision on optimized plasmonic waveguide couplers | 6 | KIT
MS26 | Fabrication of plasmonic waveguide couplers with less than 3 dB coupling loss | 12 | KIT
MS27 | Design of first generation beam shapers and compact optical filters | 12 | IMEC
MS28 | DDCM with electrical PHY design and verification | 12 | ST
MS29 | Data codecs for power consumption reduction | 15 | ST
MS30 | Decision on plasmonic waveguide couplers with less than 3 dB coupling loss | 15 | KIT
MS32 | Fabrication of compact optical filters and first generation beam shapers | 18 | IMEC
MS33 | Data codecs for error detection and correction | 18 | ST

## Slide 7: Deliverables
 | Names of the Milestones | Month | Partner
D5.1 | DDCM specification document | 6 | ST
D5.2 | DDCM with electrical PHY design and verification data base | 12 | ST
D5.3 | Compact optical filters (2nm bandwidth, >30nm FSR) and first generation beam shapers | 21 | imec
D5.4 | Generic DDCM compatible with plasmonic-based PHY specification document | 24 | ST
D5.5 | Report on plasmonic waveguide couplers | 24 | imec
D5.6 | Generic DDCM compatible with plasmonic-based PHY design and verification data base | 30 | st
D5.7 | Second generation beam shapers (distance 1mm, with bandwidth > 10nm and efficiency > 3dB) | 33 | imec

## Slide 8: Tasks
 | Names of the Tasks | Time Period [months]
Task 5.1 | Modeling and fabrication of coupling Si waveguide to plasmonic waveguide | 1 – 15
Task 5.2 | Design and fabrication of Si beamshaper | 1 – 30
Task 5.3 | Design and fabrication of passive ultra-compact components as filters | 1 – 15
Task 5.4 | Signal generation module design | 4 – 12
Task 5.5 | Signal Generation Module implementation via FPGA | 13 – 24

## Slide 9: 3D Design of the Phase Modulator
Upp=4.5V

## Slide 10: Task 5.1 - SPP Excitation in the Slot
q

## Slide 11: Task 5.1 - Fabrication by KIT & IMEC
Design

## Slide 12: Task 5.1 - Fabrication by KIT & IMEC
Si slab
Design Layout
Si nanowire
SOI chip Fabricated by IMEC
10mm

## Slide 13: Task 5.1 - Fabrication by KIT & IMEC
SEM image of the device
Si nanowire
Au
Au

## Slide 14: Task 5.1 - Optical Characterization
Light Coupling Configuration
Cut-back measurement
2dB coupling loss
per tapered coupler!

## Slide 15: Tasks
 | Names of the Tasks | Time Period [months]
Task 5.1 | Modeling and fabrication of coupling Si waveguide to plasmonic waveguide | 1 – 15
Task 5.2 | Design and fabrication of Si beamshaper | 1 – 30
Task 5.3 | Design and fabrication of passive ultra-compact components as filters | 1 – 15
Task 5.4 | Signal generation module design | 4 – 12
Task 5.5 | Signal Generation Module implementation via FPGA | 13 – 24

## Slide 16: Task 5.2 – Optical Beam Steerers
Original objective: focusing grating, distance 100mm, 5dB loss (GEN1)
New objective: develop movable gratings
        1 mm movement in plane
        1 degree rotation

## Slide 17: Task 5.2 – Optical Beam Steerers
Status:
  First generation designed
  Fabrication completed
  Characterisation on going: 1 mm lateral movement measured

## Slide 18: Tasks
 | Names of the Tasks | Time Period [months]
Task 5.1 | Modeling and fabrication of coupling Si waveguide to plasmonic waveguide | 1 – 15
Task 5.2 | Design and fabrication of Si beamshaper | 1 – 30
Task 5.3 | Design and fabrication of passive ultra-compact components as filters | 1 – 15
Task 5.4 | Signal generation module design | 4 – 12
Task 5.5 | Signal Generation Module implementation via FPGA | 13 – 24

## Slide 19: Task 5.3 – Optical filter
Goal: filter optical amplifier noise before detector
Objective: 3nm bandwidth, 10dB suppression, 30nm FSR
Activities:
Designed different types of filters (AWG, ring)
Fabricated + Characterised filters
100um
AWG
Ring

## Slide 20: Task 5.3 – Optical Filter
Device Details:
10x400 GHz AWG - size: 370x330 um2 - design FSR = 42 nm
Measurement details:
Insertion Loss: -0.90dB Non Uniformity: 0.8 dB
Crosstalk: 22 dB 3dB Bandwidth: 1.75 nm
Standard AWG

## Slide 21: Task 5.3 – Optical Filter
Flat-top AWG
Device Details:
12x400 GHz AWG - size: 560x350 um2 - design FSR = 38.2 nm
Measurement details:
Insertion Loss: 3.29dB Crosstalk: 17 dB 3dB Bandwidth: 3.30 nm

## Slide 22: Task 5.3 – Optical Filter
Double ring
Single ring
3dB Bandwidth = 0.34nm
Crosstalk <-20dB
Size: 25x25 um2
3dB Bandwidth = 1.12nm
Crosstalk <-20dB
Size: 50x25 um2

## Slide 23: Tasks
 | Names of the Tasks | Time Period [months]
Task 5.1 | Modeling and fabrication of coupling Si waveguide to plasmonic waveguide | 1 – 15
Task 5.2 | Design and fabrication of Si beamshaper | 1 – 30
Task 5.3 | Design and fabrication of passive ultra-compact components as filters | 1 – 15
Task 5.4 | Signal generation module design | 4 – 12
Task 5.5 | Signal Generation Module implementation via FPGA | 13 – 24

## Slide 24: Task 5.4 – Main achievements
DDCM functional specification completed (D5.1)
DDCM design activity completed (MS28/D5.2)
  VHDL design completed
    All features in place (STNoC support, virtual wires, Qos, credit-based flow control, PHY adapter, electrical PHY)
  Verification environment in place for both VHDL and netlist
  Full regression in place and passing
DDCM design characterization completed
  Area: around 300 Kgates
  Speed: up to 450 MHz
  PHY Tx crossing latency: 3.5 cycles at 450MHz
  PHY Rx crossing latency: 0.5 cycles at 450MHz
  Total crossing latency: 4 cycles at 450MHz i.e. 8.88ns
A patent proposal about alternative optical link proposed by ST Support Technologies Group has been submitted and is currently under evaluation by ST patent committee

## Slide 25: Task5.4 – DDCM Specification
The DDCM is composed of a transmitter (Tx) and a receiver (Rx).
The former is responsible for sending to the other die initiator requests, target responses, asynchronous events and credit information, the latter is responsible for collecting the same information from the other die.
The phisical channel is unidrectional, two channels ensure the simultaneous communication between the two dice.

## Slide 26: Task5.4 – DDCM Specification
Both DDCM transmitter and receiver are composed of a controller, composed of storage FIFOs, QoS and flow control logic, serialization and frequency conversion modules, responsible for encapsulating the system information in a format suitable to be transmitted across the physical channel, and a PHY, responsible for the actual data transmission at physical level.

## Slide 27: Task 5.4 - What’s next
Security encoder
LP encoder
EDC encoder
Serializer
Emitter/
modulator driver
Emitter/
modulator
Security decoder
LP decoder
EDC decoder
Deserializer
TIA
Detector
Traffic source
Traffic Destination
Physical channel (waveguide, fiber, free space)
Digital
Analog
Photonic
New modules to be developed include codecs for data encryption for security, codecs for reducing dynamic power consumption, and codecs for error detection and correction in case of noisy physical channel.

## Slide 28: Summary
Progress fully according to plan
Optical interfaces designed, fabricated and tested
  Coupler dielectric <> plasmonic waveguide
  Optical filters
  Optical beam shapers
Electrical interfaces designed and implemented

## Slide 29: Outlook
Task 5.1 – Couplers
  Further optimization of the process
  Next post-processing is being carried out by KIT
  New cut-back measurement
Task 5.2 – Beam shapers
  Incorporate foucssing grating on moving platform
Task 5.3 – Filters
  Completed (incorporate in final demonstrator)
Task 5.4 – DDCM specification
  Completed
Task 5.5 – DDCM implementation
  Signal Generation Module implementation via FPGA