## Slide 1
Different lengths of waveguide covered
Extraction through grating couplers or horizontal (end-facet)
Goal ?
Evaluate optical properties of hybrid nanocrystal enhanced waveguides (similar to VSL, study coupling of emission to waveguide, … )
Nanocrystal layer
Silicon rib waveguide
Pump light (532 nm)
Top-down pumping of nanocrystal enhanced Si-wg

## Slide 2
sample
Objective
Nd:YAG
Reflector
Pinhole, XY stage
Dichotic mirror
Image plane (25×)
Iris, XY stage
Mono slit
Fine focus lens, Z stage
Expander lens1, Z stage
Expander lens2
f0=100 mm
FFT
plane
f1
f3=400 mm
f2
Removable
reflector
NIR camera
NAout=0.65/25
=0.026
NAin=0.65
f=4mm
NAout=1/2/3.9
=0.128
NAin=0.026
f2/f1=0.026/0.128=0.2
f2=40 mm, f1=200 mm
f=19 mm
f=200 mm
Uniform lighting
Iris to change the size of pumping
f=100 mm
Setup

## Slide 3
Planarized Silica
Silicon rib waveguide
Development of generic integration platform
Active layer (nanocrystals, TCO’s, graphene)
Metal contact
Advantages ?
Hybrid metal-semiconductor slot allows for efficient contacting and mode confinement
Generic for modulators, detectors and light sources
Planarization removes possible side-effects and roughness
Issues ?
Alignment, conductivity of silicon waveguide