## Slide 1
Unit of Materials and Optoelectronic Devices
University of Valencia
www.uv.es/umdo

## Slide 2
Summary
2/12
1-Amplifier
2- Photodetector
3- Milestones
4- Dissemination

## Slide 3
Plasmonic Amplifiers
Dielectric waveguides (IR)
Power dependence as a function of the stripe length (PER from UGENT)
3/12
A
B
C
Narrowing for the highest PL (B)? But S/N low
A
B
C
No dependence for PbS QDs

## Slide 4
Plasmonic Amplifiers
New approaches
femptosecond Ti:Al2O3 laser: crystal to double wavelength (800nm  400 nm) already ordered
New symmetric plasmonic waveguides in the IR: we need new material from UGENT
IR CCD camera
4/12
20 µm
10 µm
8 µm
6 µm
4 µm

## Slide 5
Photodetector
5/12
200 µm
100 µm
Photomask
Lithographic process
2. Post bake 120-140 ºC
Substrate
Resist + precursor
UV Light
Photoresist
Conducting
IPN Patterns
Metal NP
Starting-point: R. Abargues, P.J. Rodríguez-Cantó, R. García-Calzada, and J. Martínez-Pastor, Patterning of Conducting Polymers using UV lithography: The in-situ polymerization approach, J. Phys. Chem C 116, 17547-17553 (2012).
In-situ synthesis of conducting polymer into the patternable host matrix
In-situ synthesis of Au NPs into the PCP -> Increase of Photoconductivity due to local heating of AuNPs
Conducting polymers

## Slide 6
Photodetector
6/12
Optical Properties
Polymerization and AuNPs generation can be followed by UV-Vis Spectroscopy
Conducting Polymer + Au NP
3T + Au (III)
TEM Characterization
Transmission Electron Microscopy (TEM) images of the multicomponent material show Au NPs dispersed in the polymer matrix. NPs diameter obtained is between 4 and 8 nm.
Conducting polymers

## Slide 7
Photodetector
7/12
Percolation Theory:
σ = σ0 (f-fc)t
So far:
- Conductivity: 10-30 S/cm
- Responsivity at 533 nm: 0.004 A/W
Conducting polymers
    QD solids (layer-by-layer method) using different ligands (MPA and EDT). MPA: 0.006 – 0.018 A/W EDT: 0.001 – 0.006 A/W
    Better dark conductivities and photocurrent with MPA due to shorter molecular distance between QDs (1.6 nm) and less surface defects.
QD solid

## Slide 8
Photodetector
8/12
Summary (conductive polymer+QDs layers)
- Needed of increase of Responsivity and EQE
- Optimization of the setup to measure photoconductivity
Optimization of electrode configuration -> 1-10 microns distance is required!!
New layout

## Slide 9
Photodetector
Final design
9/12

## Slide 10
Milestones
Demonstration of conductive QD layers with photoconductive properties
Demonstration of metal-(lithographic) polymer and QD metal-(lithographic) polymer nanocomposites
10/12
MS19:
MS18:
month 15
in progress
patent application sent

## Slide 11
Milestones
Demonstration and decision on photodetector
operation: nano-gap (MIM) vs Schottky/heterostructure
Electroluminscence from QD stack embedded within
conductive oxides (>1uW)
11/12
MS21:
MS20:
month 18
D4.1:
Designs of plasmonic amplifiers
D4.2:
Report on optical properties of QDs layers and polymer nanocomposites
design done
in progress
ok
ok

## Slide 12
Dissemination
Abstract sent to SPP: International conference on Surface plasmon photonics. (in collaboration with AIT, UGENT, IMEC)
http://www.conferium.com/WPclients/spp6/
Paper about coupling between PMMA and SU-8 waveguides to be submitted to Journal of Lightwave technology
Patent sent about prepaterning of metallic nanostructures
12/12