## Slide 1
NAVOLCHI
Unit of Materials and Optoelectronic Devices
University of Valencia
www.uv.es/umdo
Torres de Serranos (1398)
Valencia, Spain
Prof. Dr. Juan P. Martínez Pastor
Dr. Pedro Rodríguez Cantó (QD and Polymer layers, metal nanostructures)
Dr. Isaac Suárez Álvarez (Plasmonics + Optical)
Henry Gordillo (PhD student: Plasmonics + Optical)
Mari Luz Martínez (PhD student: Polymer layers, metal nanostructures)
Dr. Rafael Abargues (Chemistry, Intenanomat/Spin-Off)
Dr. Guillermo Muñoz Matutano (Optical)
(Dr.) Josep Canet Ferrer (Optical)
David Rivas Góngora (Optical)

## Slide 2
Torres de Serranos (1398)
Valencia, Spain

## Slide 3
EXPERTISE
SOI technology: photonic lens
Plasmonic nanocomposites:
nanoparticles on oxides and polymers (resists)
Quantum Optics
Single-photon Logic gates
Quantum Nanostructures for Quantum Information Technologies:
optical properties at single level

## Slide 4
Role in the project / Main Tasks
Plasmonic amplifiers by using polymers doped with QDs (embedding metal waveguides) (Task 4.3, 4.4, 5.1)
Fabrication of metal nanostructures based on patternable metal-polymer nanocomposites
Demonstration of amplification in polymer thin films / stripes
Light coupling to metal waveguides and plasmon propagation / amplification
Plasmon/Photon-Plasmon Photodetectors based on QDs and metal nanostructures (Task 4.2, 4.5)
Stacks of QDs (layer-by-layer method) for photoconductors/photodetectors
Patternable conductive polymers with added plasmonic capabilities

## Slide 5
Nanocomposite QD-Polymer dielectric waveguides
QDs incorporated in PMMA: Planar waveguides
Simple fabrication and low cost
- Appropiate concentration shows low losses
- PL coupled to waveguide modes
- Emission wavelength can be tuned
Three color waveguiding CdS,CdTe, CDSe-PMMA film
IR waveguiding
PbS-PMMA film

## Slide 6
Nanocomposite QD-Polymer dielectric waveguides
QDs incorporated in SU8: Ridge waveguides
Ligand exchange to incorporate QDs in SU8
Low losses in 0.5-1.5 µm
PL confined in 2D
- Emission wavelength tunned with material/size
CdSe-SU8 waveguide
PbS-SU8 waveguide

## Slide 7
Nanocomposite-Au plasmonic waveguides
Au film between nanocomposite and SiO2
Laser coupled to the SPP mode (TM)
PL propagated in both polarizations
Under current Work!!!
SPP GaN propagation (TM)
PL propagation (TE and TM)

## Slide 8
Coupling light in the gold nanowire with an optical fiber
Pumping QDs by end-fire coupling or from the surface
CCD camera monitors metal 1D-waveguiding
Possibility to measure the emission spectra at edge or at surface
Nanocomposite-Au plasmonic waveguides

## Slide 9
Nanocomposite Film
In-Situ synthesis of Ag/PVA nanocomposites
Patented method
Development of plasmonic metal layers by chemical growing of metal NPs: Towards prepatterned plasmonic nanostructures
Nanotechnology 19, 355308 (2008).
Plasmon resonance in ebeam patterns
Langmuir 26, 2825-2830 (2010).
3D Lithography
In-Situ synthesis of Ag(Au)/Novolac
J. Materials Chemistry 20, 7436 - 7443 (2010)

## Slide 10
t = 0
t = 3 days. Not cond.
t = 8 days. Not conductive
t = 21 days. Conductive
Increase of LSPR with growth time:
Increase of size + density of Nanoparticles
Nanocomposite Film
In-Situ synthesis of the Au/Novolac nanocomposite
Patented method
Patent pending
Development of plasmonic metal layers by chemical growing of metal NPs: Towards prepatterned plasmonic nanostructures

## Slide 11
Development of layer stacks containing IV-VI QDs
Oleyamin-capped PbS QDs
QD monolayer
QD multilayer
QD monolayer
Spincoating
Ethanedithiol
HS-CH2-CH2-SH
Ligand Exchange
LbL
LiF
ITO
Device Fabrication
- Simple low-T processing
Wide variety of materials
High control of the thickness
Layer-by-Layer approach
to fabricate photodetectors

## Slide 12
Development of layer stacks containing IV-VI QDs:
Photocurrent Measurements

## Slide 13
Development of layer stacks containing IV-VI QDs:
Film Characterization
TEM
XPS
OA-capped PbS
After EDT treatment

## Slide 14
Photomask
Lithographic process
2. Post bake 120-140 ºC
Substrate
Resist + precursor
UV Light
Photoresist
Conducting
IPN Patterns
In-situ synthesis of conducting polymer into the patternable host matrix
Possibility of in-situ synthesis of Au NPs into the PCP
Possibility of easy incorporation of QDs into or on top of the PCP
Development of Patternable Conductive Polymers
40 µm
20 µm
200 µm
100 µm
Manuscript submitted to the Journal of Materials Chemistry (Jan, 2012)

## Slide 15
Perspectives in the project
Selectively functionalized surfaces to deposit homogenous monolayers of nanoparticles (QDs, metal)

## Slide 16
Next Perspectives/Objectives
Plasmonics amplifiers (tasks 4.1,4.3,4.4 and 5.1)
Gain/Amplification in dielectric waveguides
Light coupling to metal nanowires/1D-waveguides
SPP propagation and amplification in gold waveguides
Modelling (AIT)
Core-shell PbS/PbSe (U. Ghent)
Photon-Plasmon Photodetectors (tasks 4.2,4.5 and 5.1)
- QD-LbL
- Conducting polymer