## Slide 1
Work Package 4 Presentation
Juan P. Martínez Pastor
University of Valencia (UVEG), Spain

## Slide 2
WP3 Position in Project
Objectives
Tasks
Milestones and Deliverables
Status of Work
  Task 4.1. Design and modelling of Plasmonic Amplifier
  Task 4.3. Colloidal QDs for gain
  Task 4.4. QD-based Plasmonic Amplifier
  Task 4.5. QD-based Photodetectors
Summary and Outlook
Outline

## Slide 3
WP4 Position in Project
Contributors:

## Slide 4: Tasks
 | Names of the Tasks | Time Period [months]
Task 4.1 | Design and modeling of plasmonic pre-amplifier | 1 – 18
Task 4.2 | Design and modeling of plasmonic photodetector | 1 – 24
Task 4.3 | Colloidal quantum dots with optimized gain and electrical injection scheme | 1 – 18
Task 4.4 | Fabrication and characterization of QD-based plasmonic amplifiers | 6 – 30
Task 4.5 | Fabrication of plasmonic polymer QD based photodetectors | 1 – 36

## Slide 5
Objectives
Simulation studies to optimize
  Plasmonic amplifier
  Plasmon/Photon detector
Fabrication
  Optically pumped plasmonic amplifier
  Electrically driven plasmonic amplifier
  Plasmon/Photon detector
Performance targets
  Plasmonic amplifier: 10 dB on-chip gain (5 mm wide)
  Detector: Responsivity > 1 A/W (EQE ≈ 80 %)

## Slide 6: Milestones
 | Names of the Milestones | Month | Partner
MS16 | Decision on optimized structures for plasmonic amplifiers | 12 | UVEG
MS17 | Synthesis of nanoparticles with gain at 1550nm | 12 | UGENT
MS18 | Demonstration of conductive QD layers with photoconductive properties | 15 | UVEG
MS19 | Demonstration of metal-(lithographic) polymer and QD metal-(lithographic) polymer nanocompo-sites | 15 | UVEG
MS20 | Demonstration and decision on photodetector operation: nano-gap (MIM) vs. Schottky / heterostructure | 18 | UVEG
MS21 | Electroluminescence from QD stack embedded within conductive oxides (>1µW) | 18 | IMCV
MS22 | Demonstration of plasmonic amplifiers with optical pumping exhibiting 10dB gain | 21 | IMCV
MS23 | Operation of QD based photodetector with responsivity > 0.1 A/W | 24 | UVEG
MS24 | Demonstration of SPP amplifiers with electrical injection exhibiting 10dB/cm gain | 30 | UVEG

## Slide 7: Deliverables
 | Names of the Deliverables | Month | Partner
D4.1 | Designs of plasmonic amplifiers | 18 | UVEG
D4.2 | Report on optical properties of QDs layers and polymer nanocomposites | 18 | UVEG
D4.3 | Designs of plasmonic photodetectors | 24 | UVEG
D4.4 | Report on SPP amplifiers by using QDs | 30 | IMEC
D4.5 | Report on plasmonic photodetectors | 33 | UVEG

## Slide 8
Task 4.1 Design&Modelling of P.A.
Asymmetric
    t = 30 nm is a good compromise
    Symmetric design has SPP solution in the entire t-range
Optimizing design for LR-SPP propagation: Au thickness
Symmetric
Reported on MS16
NO GAIN

## Slide 9
Task 4.1 Design&Modelling of P.A.
Optimizing design for LR-SPP propagation: cladding layers
    d = d1 = d2 < 3 mm
    Propagation length decreases for d < 4 mm
    LR-SPP extends > 3 mm
    High order modes appear
Reported on MS16

## Slide 10
MOST PROMISING MATERIALS FOR GAIN: PbS/CdS (PBSe/CdSe) rods
Task 4.3 Colloidal QDs with gain …
    Synthesis of heterostructured core-shell quantum nanorods:
    Tunable IR lem
    High quantum yield = 45- 55 %
Reported on MS17
CdS
PbS
PbS/CdS Partially Exchanged Rods
PbS/CdS Partial Exchange Rod material
    PL
    ABSORPTION
Y. Justo, B. Goris, J. S. Kamal, P. Geiregat, S. Bals, and Z. Hens, JACS 2012, 134, 5484-5487.

## Slide 11
Task 4.3 Colloidal QDs with gain …
Reported on MS17
    Rod-shaped PbS do cross the transparency threshold under high occupation (45 excitons per rod)
MOST PROMISING MATERIALS FOR GAIN: PbS/CdS (PBSe/CdSe) rods

## Slide 12
Gain measured on dielectric films doped with Q-nanorods
Task 4.3 Colloidal QDs with gain …
    Characterization of gain material in PMMA by Variable Stripe Length method
    Rate equation model for interpretation of guided PL: saturated gain + losses
I. Suárez, H. Gordillo, R. Abargues, S. Albert, and J. Martínez-Pastor, Photoluminiscence wave-guiding in CdSe and CdTe QDs-PMMA nanocomposite films, Nanotechnology 22, 435202 (2011).
Detection system
Mycroscope objective
Polarizer

## Slide 13
Task 4.3 Colloidal QDs with gain …
    Best Gain/losses ratio in PbS/CdS PER
    High gain in 300 mm of pumping stripe
    Gain saturation due to Auger mechanism
Reported on MS17
ldet
ldet
Gain measured on dielectric films doped with Q-nanorods

## Slide 14
QDs in SU-8 for fabricating Plasmonic Amplifier
Task 4.3 Colloidal QDs with gain …
    QDs incorporated in SU-8 by ligand exchange
    Demonstrated the fabrication of 4-20 mm wide stripes.
    Different QDs (CdSe, PbS)
H. Gordillo, I. Suárez, R. Abargues, P. Rodríguez-Cantó, S. Albert and J.P. Martínez-Pastor, Polymer/QDs nanocomposites for wave-guiding applications, Journal of Nanomaterials, Vol. 2012, Article ID 960201 (doi:10.1155/2012/960201), 1-9 (2012).

## Slide 15
At beginning of Positive voltage pulse
At end of positive voltage pulse
Task 4.3 Colloidal QDs with gain …
QD layers for electrically driven PA
    AC electroluminescence concept
    Compatible with Si-technology
V. Wood, M. J. Panzer, D. Bozyigit, Y. Shirasaki, I. Rousseau, S. Geyer,
M. G. Bawendi, and V. Bulovic, Electroluminescence from Nanoscale Materials via Field-Driven Ionization, Nano Lett. 2011, 11, 2927–2932

## Slide 16
Task 4.3 Colloidal QDs with gain …
QD layers for electrically driven PA
    AC electroluminescence is identical to PL
    Efficiencies are 0.14 lumen/watt
Wavelength [nm]
Normalized Intensity

## Slide 17
Task 4.4 Fabrication of QD-based PA
Fabrication of optically pumped Plasmonic Amplifier
    TM, TE are plasmonic/photonic hybrid modes
    Gain and losses are similar to those measured in pure dielectric modes
    Symmetric structure under preparation

## Slide 18
Interaction Length [mm]
Power Difference [dBm]
Task 4.4 Fabrication of QD-based PA
    QDS interact with the optical mode of the waveguide
    Losses increase after AlOx and ITO
Fabrication of Electrically driven Plasmonic Amplifier

## Slide 19
Task 4.5 Fabrication of Photodetector
Photodetection based on QD layers
    QD solids (layer-by-layer method) using different ligands (MPA and EDT).
    Better dark conductivities and photocurrent with MPA due to shorter molecular distance between QDs (1.6 nm) and less surface defects.
A
External Quantum Efficiency (%)
10
1
0.1
MPA ligand
(3-mercaptopropionic acid)
EDT ligand
(1,2-ethanedithiol)
Responsivity
MPA: 0.006 – 0.018 A/W
EDT: 0.001 – 0.006 A/W
ITO
d = 130 nm

## Slide 20
200 µm
100 µm
Photomask
Lithographic process
2. Post bake 120-140 ºC
Substrate
Resist + precursor
UV Light
Photoresist
Conducting
IPN Patterns
Metal NP
Photodetection based on conductive polymers
    Demonstrated conductive 3T(*) with Cu(ClO4)2 inside Novolak.
    Demonstrated conductive 3T(*) with HAuCl4 + formation of Au NPs in PMMA.
R. Abargues, P.J. Rodríguez-Cantó, R. García-Calzada, and J. Martínez-Pastor, Patterning of Conducting Polymers using UV lithography: The in-situ polymerization approach, J. Phys. Chem C 116, 17547-17553 (2012).
Task 4.5 Fabrication of Photodetector
Conductivity: 10-30 S/cm
Responsivity at 533 nm: 0.006 A/W at 10 V
(*)3T: Terthiophene

## Slide 21
Materials: Optimize hetero-nanostructures emitting at 1550 nm
Polymer-based PA: Corroborate experimentally conclusions on MS16 (symmetric design) and begin with on Au-2D waveguides (+ design)
Hybrid-Si PA: Design, fabrication and characterization of electrically driven structures
Plasmonic Amplifier:
Design of optimized structures for plasmonic amplification
Hetero-nanostructures emitting at the infrared with high quantum yield have been synthesized:
- High gain in cladding layers for optical pumping concept
- AC Electrical driven concept
Fabrication of optical and electrical driven plasmonic amplifiers
Photodetector:
Photoconductors based on QD-layers
Photoconductors based on polymers interpenetrated in patternable polymers
Summary and Outlook
Outlook
Summary
Photodetectors: Design, fabrication and characterization of structures