## Slide 1
Work Package 3 Presentation
“Project NAVOLCHI”
Victor Dolores-Calzadilla, Meint Smit
Eindhoven University of Technology (TU/e), The Netherlands

## Slide 2
WP3 Position in Project
Objectives
Tasks
Milestones and Deliverables
Status of Work
  Task 3.1. Modeling of plasmonic laser
  Task 3.2. Modeling of plasmonic modulator
  Task 3.3. Fabrication of plasmonic/metallic laser
  Task 3.4. Fabrication of Si-plasmonic modulators
Summary and Outlook
Outline

## Slide 3
WP3 Position in Project
Contributors:

## Slide 4
Objectives
Simulation studies
  Plasmonic/metallic nanolaser
  Plasmonic modulator
Fabrication
  Electrically pumped plasmonic/metallic nanolaser
  Electrically driven plasmonic modulator
Performance targets
  Laser: active region < 1 mm2, output power > 100 mW
  Modulator: extinction ratio > 3dB for length < 10 mm, and a total modulation speed > 40 Gbit/s

## Slide 5: Tasks
 | Names of the Tasks | Time Period [months]
Task 3.1 | Modelling of plasmonic laser and optimization of bonding technology | 1 – 6
Task 3.2 | Modelling of plasmonic modulator | 1 – 18
Task 3.3 | Fabrication of plasmonic/metallic nanolaser | 7 – 30
Task 3.4 | Fabrication of Si-plasmonic modulators | 7 – 27

## Slide 6: Milestones
 | Names of the Milestones | Month | Partner
MS8 | Decision on an optimized structure for metallic/plasmonic nanolaser and its coupling to a Si-waveguide | 6 | TU/e
MS9 | Decision on an optimized structure for plasmonic modulator | 6 | KIT
MS10 | Grown wafer structure for plasmonic lasers | 12 | TU/e
MS11 | Fabrication of plasmonic modulator on a SOI platform | 15 | KIT
MS12 | Decision on an optimized structure for plasmonic modulator with a maximum loss of 20dB | 18 | KIT
*MS13 | Initial characterization of unbonded plasmonic lasers | 18 | TU/e
MS14 | Initial testing and characterization of plasmonic modulators | 21 | KIT
MS15 | Initial testing of bonded plasmonic lasers | 24 | TU/e
*MS13 has been identified as inappropriate to the course of the project and was skipped in agreement with EC

## Slide 7: Deliverables
 | Names of the Deliverables | Month | Partner
D3.1 | Report on studies of optimized structure for metallic/plasmonic nanolaser and its coupling to Si-waveguide | 12 | TU/e
D3.2 | Report on modelling of the modulator structure | 12 | KIT
D3.3 | Fabrication of plasmonic laser device | 24 | TU/e
D3.4 | Report on fabrication of modulators | 24 | KIT

## Slide 8: Task 3.1 Modelling of the Nanolaser
Fabry-Perot plasmonic laser [1]
  High propagation loss and poor active confinement
Reported in D3.1
xy
|E|2
|E|2
[1] V. Dolores-Calzadilla, et al., ICTON 2012.
[2] V. Dolores-Calzadilla, et al., ICTON 2013.
Metallo-dielectric nanolaser [2]

## Slide 9
Task 3.3 Fabrication of the Nanolaser
Technology development
III-V wafer bonding to Si-substrate
Low-loss Au/Ag/Ge contacts[1][2]
Silver-deposition and treatment
Nanopillar on waveguides
[1] L. Shen, et. al., Optical Materials Express 5(2), 2015.
[2] L. Shen, et. al., Optical Materials Express (submitted), 2015.
Reported in D3.3 & FR

## Slide 10
Task 3.3 Fabrication of the Nanolaser
[1] V. Dolores-Calzadilla, et. al., Nature Communications (to be submitted)
Complete fabrication on III-V/Si [1]

## Slide 11
Task 3.3 Fabrication of the Nanolaser
Reverse bias current: 0.5 µA
Minimum FWHM: 25 nm (Q~62)
Max. power: 60 nW
Max. on-chip Ext. Quantum Eff.: 10-2
State-of-the-Art: pW, 10-7 – 10-5 [1,2]
Static characteristics: LED operation
Reported in FR
[1] Shambat, et. al., Nature Communications 2, 2011.
[2] Huang, et. al., Nature Photonics 8, 2014.
Record value

## Slide 12
Task 3.3 Fabrication of the Nanolaser
Electrical pulses: 1 ns to 100ps sub-ns response
Due to strong non-radiative recombination
  Modulation depth:
  96% at 2 GHz
  42% at 5 GHz
Dynamic characteristics: LED operation

## Slide 13
Task 3.3 Fabrication of the Nanolaser
Time-resolved photoluminescence of nanopillars
  Surface recombination velocity S ~ 1x105 cm/s
  Strong surface recombination!

## Slide 14
Task 3.3 Fabrication of the Nanolaser
Redesign: micro-cavity, undercut, whispering gallery mode
M | Radius | Q-factor |  | Confinement |  | 
4 | 500 | 1149 | 1533 | 0.35 | 0.12 | 0.03
5 | 625 | 2094 | 1583 | 0.35 | 0.095 | 0.01
M | Radius | Q-factor |  | Confinement |  | 
4 | 500 | 1149 | 1533 | 0.35 | 0.12 | 0.03
5 | 625 | 2094 | 1583 | 0.35 | 0.095 | 0.01
Different stress
More fragile

## Slide 15
Summary and Outlook (Light Source)
  Summary
    Modelling of waveguide-coupled metal-cavity nanolasers
    Technology development of metal-based devices in III-V/Si
    Fabrication completed and LED operation observed:
      Max. output power: 60 nW
      Max. on-chip EQE: 1%
      Switching speed up to 5 GHz
  Outlook
    Publish main results in journal paper
    Realize passivation studies for future nanoscale sources
    Use silver-based ohmic contacts in TUe’s membrane technology

## Slide 16: Task 3.2 Modelling of the Modulator
Reported in MS9 & D3.2
SPP absorption modulator
SPP phase modulator

## Slide 17
Ultra-fast
Instantaneous Pockels effect:
Small RC-time constant
Ultra-compact
Enhanced nonlinearity
Perfect overlap
Energy-efficient
Small Vp & small capacitance
Concept
Disadvantage: High losses
Task 3.4 Fabrication of the Modulator
A. Melikyan et al., "High-speed plasmonic phase modulators," Nature Photon. 8(2), 229–233 (2014).
Phase Modulator

## Slide 18
Task 3.4 Fabrication of the Modulator
A. Melikyan et al., "High-speed plasmonic phase modulators," Nature Photon. 8(2), 229–233 (2014).
Phase Modulator
Passive silicon-on-insulator (SOI) wafer processing
E-beam lithography for defining 140 nm wide slot in gold
Coating with an electro-optic polymer
Poling of electro-optic polymer with static electric field
Reported in MS11

## Slide 19
Vm = 0.8 V
r33 ≈ 21 pm / V
VpL = 1.3 Vmm
Vm = 0.1 V
A. Melikyan et al., "High-speed plasmonic phase modulators," Nature Photon. 8(2), 229–233 (2014).
Task 3.4 Fabrication of the Modulator
Broadband optical operation across 120nm (fm = 45GHz)
65 GHz RF bandwidth (lc = 1.55mm)
Phase Modulator

## Slide 20
Task 3.4 Fabrication of the Modulator
A. Melikyan et al., "High-speed plasmonic phase modulators," Nature Photon. 8(2), 229–233 (2014).
Phase Modulator

## Slide 21
Task 3.4 Fabrication of the Modulator
C. Haffner et al., “All-plasmonic Mach-Zehnder modulator enabling optical high-speed communication at the microscale”, Nature Photonics 9, 525 – 528 (2015)
Length 10 µm
Voltage-length poduct 60 Vµm
Energy consumption 25 fJ/bit
Insertion loss 8 ±1 dB
All-Plasmonic MZM Modulator

## Slide 22
Unique footprint of an IQ Modulator: 750mm2
Task 3.4 Fabrication of the Modulator
Haffner, et al., in Optical Communication (ECOC), 2015 European Conference on(2015).
All-Plasmonic IQ Modulator

## Slide 23
1st Gen. – QPSK – 120 Gbit/s – 143 fJ/Bit
– 16QAM – 60 Gbit/s – 27 fJ/Bit
2nd Gen. – QPSK – 72 Gbit/s – 78 fJ/Bit
IL 21.5 dB
IL 13.5dB
Task 3.4 Fabrication of the Modulator
Haffner, et al., in Optical Communication (ECOC), 2015 European Conference on(2015).
All-Plasmonic IQ Modulator
Notes: Bias applied
QPSK – 72 GBd – BER 7.5x10-3 15um/40nm
16QAM -18 GBd –BER 1.3x10-2 15um/85nm
BER 1.3x10-5 11um/85nm

## Slide 24
100 µm
Si
Au
CW in
Modulated out
ϑ
G
S
G
-ϑ
Task 3.4 Fabrication of the Modulator
W. Heni, et al., J. Lightwave Technol., in press (2015).
Melikyan et al., ,Optics Express, Vol. 23, Issue 8, pp. 9938-9946 (2015)).
MZM Modulator
Notes: Ground-signal-ground configuration. Phase shift ϑ in two arms in opposite direction  push-pull
V_piL (Wolfgang): 90Vµm, Vpi=3.4 V, r33=160 pm/V

## Slide 25
100 µm
Si
Au
CW in
Modulated out
ϑ
G
S
G
-ϑ
Task 3.4 Fabrication of the Modulator
MZM Modulator
108 Gbit/s 4-PAM
W. Heni, et al., J. Lightwave Technol., in press (2015).
Melikyan et al., ,Optics Express, Vol. 23, Issue 8, pp. 9938-9946 (2015)).
Notes: Ground-signal-ground configuration. Phase shift ϑ in two arms in opposite direction  push-pull
V_piL (Wolfgang): 90Vµm, Vpi=3.4 V, r33=160 pm/V

## Slide 26: Summary and Outlook (Modulator)
  Summary
    Different plasmonic phase and Mach-Zehnder modulators have been successfully demonstrated
Bandwidth > 65 GHz
Broadband optical operation: Dl > 120 nm
Data transmission up to 72 Gbit/s
  Application areas
    Short-reach interconnects
    WDM backbone (WDM + QAM formats + high symbol rates)