## Slide 1
Work Package 5 Presentation
“Project NAVOLCHI”
Dries Van Thourhout
imec, Belgium

## Slide 2
WP5 Position in Project
Objectives
Tasks
Milestones and Deliverables
Status of Work
  Task 5.2: Beamshapers
Summary and Outlook
Outline

## Slide 3
WPX Position in Project
Contributors:

## Slide 4: Objectives
Overall Objective :
Specific Objectives:
  Coupling light between silicon backbone and plasmonic devices
  Beam Shaping grating couplers to direct light between chips
  Compact filters for noise suppression
  Specify and implement Dual Die Communication Module (DDCM)
Design and implement optical and electrical interfaces for plasmonic interconnect

## Slide 5: Tasks
 | Names of the Tasks | Time Period [months]
Task 5.1 | Modeling and fabrication of coupling Si waveguide to plasmonic waveguide | 1 – 15
Task 5.2 | Design and fabrication of Si beamshaper | 1 – 30
Task 5.3 | Design and fabrication of passive ultra-compact components as filters | 1 – 15
Task 5.4 | Signal generation module design | 4 – 12
Task 5.5 | Signal Generation Module implementation via FPGA | 13 – 24
Completed & Reported month 36
Completed & Reported month 36
Completed & Reported month 36
Completed & Reported month 36

## Slide 6: Milestones
 | Names of the Milestones | Month | Partner
MS25 | Decision on optimized plasmonic waveguide couplers | 6 | KIT
MS26 | Fabrication of plasmonic waveguide couplers with less than 3 dB coupling loss | 12 | KIT
MS27 | Design of first generation beam shapers and compact optical filters | 12 | IMEC
MS28 | DDCM with electrical PHY design and verification | 12 | ST
MS29 | Data codecs for power consumption reduction | 15 | ST
MS30 | Decision on plasmonic waveguide couplers with less than 3 dB coupling loss | 15 | KIT
MS32 | Fabrication of compact optical filters and first generation beam shapers | 18 | IMEC
MS33 | Data codecs for error detection and correction | 18 | ST

## Slide 7: Milestones
 | Names of the Milestones | Month | Partner
MS33 | Design of second generation beam shapers | 24 | imec
MS34 | Generic DDCM compatible with plasmonic-based PHY | 24 | ST
MS35 | Fabrication of second generation beam shapers | 39 | imec
MS36 | DDCM evolution for NiP solutions | 39 | ST

## Slide 8: Deliverables
 | Names of the Milestones | Month | Partner
D5.1 | DDCM specification document | 6 | ST
D5.2 | DDCM with electrical PHY design and verification data base | 12 | ST
D5.3 | Compact optical filters (2nm bandwidth, >30nm FSR) and first generation beam shapers | 21 | imec
D5.4 | Generic DDCM compatible with plasmonic-based PHY specification document | 24 | ST
D5.5 | Report on plasmonic waveguide couplers | 24 | imec
D5.6 | Generic DDCM compatible with plasmonic-based PHY design and verification data base | 39 | st
D5.7 | Second generation beam shapers (distance 1mm, with bandwidth > 10nm and efficiency > 3dB) | 39 | imec

## Slide 9: Task 5.2 – Optical Beam Steerers
Original idea for demonstrator:
Vertical coupling between chips
Need for free space beam couplers
  Design reveals this approach is limited in density
Updated demonstrator:
Coupling with high-density multi-core fiber (MFC)
Remaining person power devoted to innovative grating couplers
  Metal grating coupler for InP-membrane platform
  Coupler for SiN-QD platform

## Slide 10: Task 5.2: Coupling through MCF
4 out of 19 channels with 50 µm pitch
Crosstalk measured to be below -31 dB
Allows for optical amplifier between transmitter and receiver
Scalable to very high bandwidth density
Evaluation coupling & XT performance
Chiral Photonics (PROFA)

## Slide 11: Task 5.2 – Optical Beam Steerers
Chart: Distance between chips [um]
| 10.0 | 30.0 | 100.0 | 300.0 | 700.0 | 1000.0
Grating = 4um | 15.8789 | 38.3309 | 123.7498 | 370.1703 | 863.4735 | 1233.4913
Grating = 8um | 20.9293 | 27.2455 | 64.8344 | 186.0955 | 432.1708 | 617.0496
Grating = 12um | 30.2804 | 32.4367 | 50.8964 | 126.941 | 289.3645 | 412.2433
Grating = 16um | 40.1187 | 41.0558 | 50.5062 | 100.7863 | 219.5288 | 310.9462
Grating = 20um | 50.0608 | 50.5447 | 55.7545 | 89.3143 | 179.7761 | 251.7062
Grating = 24um | 60.0352 | 60.3161 | 63.4241 | 86.0436 | 155.9101 | 214.1521
Grating = 28um | 70.0222 | 70.1993 | 72.1837 | 87.7178 | 141.8239 | 189.6022
Grating = 32um | 80.0149 | 80.1336 | 81.4722 | 92.4093 | 134.3437 | 173.7006
Grating = 36um | 90.0104 | 90.0939 | 91.0375 | 98.9467 | 131.5429 | 163.9595
Grating = 40um | 100.0076 | 100.0684 | 100.7578 | 106.6267 | 132.1169 | 158.7892
Optimum | 15.8789 | 27.2455 | 50.5062 | 86.0436 | 131.5429 | 158.7892
Chart: Distance between chips [um]
| 10.0 | 30.0 | 100.0 | 300.0 | 700.0 | 1000.0
Grating = 4um | 11.7488 | 21.0313 | 62.478 | 185.2877 | 431.8236 | 616.8065
Grating = 8um | 20.2363 | 22.0359 | 36.7543 | 94.6461 | 216.7785 | 309.0106
Grating = 12um | 30.0704 | 30.6274 | 36.3677 | 68.5821 | 146.9965 | 207.7526
Grating = 16um | 40.0297 | 40.2665 | 42.8686 | 61.1512 | 115.1009 | 159.2856
Grating = 20um | 50.0152 | 50.1367 | 51.4989 | 62.2034 | 99.7741 | 133.094
Grating = 24um | 60.0088 | 60.0792 | 60.8741 | 67.4602 | 93.6856 | 119.018
Grating = 28um | 70.0055 | 70.0499 | 70.5523 | 74.8238 | 93.2926 | 112.5267
Grating = 32um | 80.0037 | 80.0334 | 80.3706 | 83.2759 | 96.499 | 111.0989
Grating = 36um | 90.0026 | 90.0235 | 90.2605 | 92.318 | 101.9847 | 113.118
Grating = 40um | 100.0019 | 100.0171 | 100.19 | 101.6972 | 108.9207 | 117.4883
Optimum | 11.7488 | 21.0313 | 36.3677 | 61.1512 | 93.2926 | 111.0989
optimum
optimum
a) Standard grating
b) Focussing grating

## Slide 12
Metal grating coupler
Metal grating coupler [1,2]
[1] V. Dolores-Calzadilla, et. al., Optics Letters 39(9), 2014.
[2] A. Higuera-Rodriguez, et. al., Optics Letters 40(12), 2015.
Performance independent from buffer thickness
Enables high yield (thick) bonding
Reduce optical parasitics into buffer/substrate
Efficiency: 54%
Reported in MS51

## Slide 13: SiN-QD Grating Couplers: Concept
Aim: develop grating coupler to couple light from SiN-QD platform
From micro-sources and/or single photon emitters
Pump beam
QD-emission
SiN with QD-embedded

## Slide 14: Parameters involved in simulation
Structure definition and parameters:
  Grating periodicity (period length and number)
  Cladding layer thickness
  Grating etching depth; Filling factor;
  Reflection layer(gold mirror or distributed bragg reflector(DBR))
SiNx
Mode source
Grating period
air
air
Etching depth
Gold mirror
Si substrate
Cladding layer thickness
etched
Filling factor=1-etched/period
Notes: To evaluate the performance of grating coupling, we measure the coupling into the fiber, divided by the overall upgoing power.
The period at 0.405μm will achieve high coupling efficiency. the bandwidth is about 25nm.
The step of silica cladding is 0.05μm, the upgoing power will achieve a maximum every 0.2μm.
The coupling efficiency can be achieved 37.3%. The bandwidth is also expand to 40nm

## Slide 15: 2D&3D Simulation SiN-QD Grating Coupler
Influence of Grating Height
Number of Periods
Up to 90% efficiency realistic (with bottom mirror)

## Slide 16: Fabrication
30μm
After etching
Initial process:
Stiction to surface
Optimised process:
No stiction
(tensile strained SiN, CPD)

## Slide 17: Comparison with simulation
Measurement, compared with optimized simulation
ff=0.5 for simulation,
ff=0.6 for fab.
Notes: Measurement 5: couple in period 560nm; filling factor(0.6)
Measurement 1: couple in period 530nm; filling factor(0.6)

## Slide 18
Summary
All WP5 tasks completed successfully
  Efficient couplers silicon waveguide – plasmonic modulators demonstrated (<1dB loss)
  Compact filters with controllable properties demonstrated
  Electrostatically actuated grating couplers demonstrated
  Grating coupler for SiN-QD and InP-membrane platforms demonstrated
  Electrical interfaces designed and implemented in STNoC

## Slide 19
Outlook & Exploitation
Efficient couplers silicon waveguide to plasmonic modulators demonstrated:
  See WP3
Compact filters with controllable properties:
  Design know-how transferred to Luceda (IMEC spin off in photonic CAD software)
Electrostatically actuated grating couplers:
  Discussion with company on implementing Silicon Photonics MEMS in large-scale switch (on-going)
Grating coupler for SiN-QD platform:
  New work towards single photon sources
Metal Grating coupler for InP-membrane platform:
  Grating coupler implemented in IMOS-platform