## Slide 1
Dielectric and plasmonic CdSe-PMMA waveguides
CdSe-PMMA waveguides
Maximum gain obtained of to 20 cm-1, but losses around 30 cm-1
Close to amplification but it needs more powerful laser or more efficient nanostructures
Similar spectra with and without gold

## Slide 2
PbS/CdS-PMMA waveguides
Broad band with emission between 1100 and 1600 nm
High stokes-shift
Good efficiency
PbS-CdS quantum rods developped by UGENT

## Slide 3
Quantum rods-PMMA nanocomposites
PbS/CdS-PMMA waveguides
filling factor | 404 nm | 633 nm | 1060 nm | waveguided PL
8·10-4 | yes | yes | yes | no
8·10-3 | no | yes | yes | yes
4·10-2 | no | no | no | yes

## Slide 4
Pumping power dependence
PbS/CdS-PMMA waveguides
Low concentration shows saturation due to the filling of quantum dots states, but a higher concentration is close to amplify!!

## Slide 5
Gain and losses characterization
PbS/CdS-PMMA waveguides
Increase of gain/losses with ff due to QD emission/reabsorption and scattering
Gain
Losses

## Slide 6
New approaches
Increase QR concentration (with the expenses of optical losses)
Pumping with a high power Nd:Yag laser (1060 nm)
to get amplification
Plasmonic waveguide
Deposite nanocomposite on a gold film
Stripe to improve confinement

## Slide 7
Papers and conferences
Poster presentation at ECIO conference (17-20 april)
ICTON paper submitted (in collaboration with AIT)
Emmanouil Panagiotis (AIT) will visit our labs nest week