## Slide 1: Navolchi Telco – 7 May 2012 Part 1 : Beam Steering
Sukumar Rudra, Dries Van Thourhout, Kasia Komorowska

## Slide 2: Beam steering
Proposed structure: grating coupler on movable MEMS platform
3 electrodes allow applying force in 3 directions
Comsol simulation
Back pad actuation
Side pad actuation

## Slide 3: Beam steering
Processing:
  Underetching initially not controllable – currently OK
Fiber Characterisation:
  Change in power + central wavelength measured when applying voltage
  Device dependent (sometimes increase, sometimes decrease)
  Change not in line with predictions
Back pad
Side pad

## Slide 4: Beam steering
Measurements using Laser Doppler Vibrometry
  Gives image of displacement
  No difference seen between side and back pad actuation
  Always tilt to front – Discrepancy with fiber based measurements
Green = low -- Red = High
Next step
  Reprocessing current samples
  Designed new version with simpler structure
Back pad
Side pad

## Slide 5: Navolchi Telco – 7 May 2012 Part 2 : Amplifier: current injection
Floris Tailleu, Kasia Komorowska, Pieter Geiregat, Zeger Hens, Dries Van Thourhout
Physics and Chemistry of Nanostructures Group

## Slide 6: Two ways of inducing e-h recombination in the QDs
Direct charge injection
Field-driven ionization (“isoLED”)
1
2
DC voltage
up to 10 V
AC voltage
up to 100 V
peak to peak
Alumina
ALD

## Slide 7: Current-voltage characteristic by direct charge injection
1
  Multiple reasons for unsuccessful measurements and irreproducibility
  High concentration of free carriers
    Quenching of the electroluminescence by non-radiative processes (especially Auger)
    Could be solved by adding an insulating layer between the quantum dots and the electron transport layer (ETL)
  Charging of the quantum dot layers
    Imbalance of number of injected electrons and holes
    Could be solved by adding an insulating layer in the ETL:
    Wide band gap material induces additional energy barrier for the electrons
  Repeated IV-measurements on same sample
No successful light emission have been measured

## Slide 8: Field-driven ionization: theoretical approach
2
                Influence of
                external electric field
                Influence of
                remaining internal field

## Slide 9: IsoLED electroluminescence results
Applied block pulse (20 kHz) at Vpp = 100 V and corresponding EL intensity
Resulting EL spectrum
Good correspondence
with PL spectrum
2
Persistent light emission, clearly visible by eye