## Slide 1
PbS/CdS-PMMA waveguides
PbS/CdS Quantum rods developped by UGent:
- Broad band: 1100-1600 nm
- Good efficiency and Stokes-shift
Plasmonic and dielectric QR-PMMA waveguides
1

## Slide 2
PbS/CdS-PMMA waveguides
Dielectric waveguides
QR mixed in PMMA with different concentrations
Good results with highest (filling factor): linear slope and g≈15 cm-1
But not enough to obtain amplification:
Experiments with doubled Nd:Yag laser developing the set-up
with higher filling factors in contact with Gent to obtain more material
2

## Slide 3
PbS/CdS-PMMA waveguides
Plasmonic waveguides
PL characterization:
Saturation of the PL with the highest concentration used (ff=0.04)
Low gain in the order of 3 cm-1
Low signalDifficult to obtain resolution with polarization
new samples will be necessary (in contact with Gent to obtain more material)
3

## Slide 4
Plasmonic waveguides
SPP Propagation length
propagation losses=f(propagation length) in TE and TM
A first fast slope in TM should be the SPP
SPP propagates only in TM
Photonic modes in TE and TM
How can we separate SPP contribution ?
In colaboration with E. Panagiotis (AIT)
But...
it has to be enough signal in TE and TM
it has to be enough resolution to see the decay of SPP
4

## Slide 5
Plasmonic waveguides
SPP Propagation length
Preliminary results in a CdSe-PMMA plasmonic waveguide
In colaboration with E. Panagiotis (AIT)
E. Panagiotis is simmulating the structures
5