## Slide 1: Navolchi Telco – 4 June 2012
(including input UGent

## Slide 2: Summary
1) Characterisation of interaction QDOTS with silicon waveguide
2) Build proposed amplifier with different top contacts
3) Preparing new QDOTS for Valencia
4) New QDOT-gain characterization planned (collaboration with TUDelft)

## Slide 3
Top electrode
Gold Contact Pad
Silicon waveguide
SiO2
Quantum Dots
Al2O3
Total stack thickness is approximately 90nm

## Slide 4: Using ITO top-contact
Qd/al2o3/ito – al2o3/ito
Absorption of PbS in solution

## Slide 5: Using ITO as top contact
ITO only
ITO + QDOTS
Difference
Clear effect of QDOTS, absorption ± 200/cm