## Slide 1
Unit of Materials and Optoelectronic Devices
University of Valencia
www.uv.es/umdo

## Slide 2
Summary
2/9
1-Amplifier
2- Photodetector
3- Milestones
4- Dissemination

## Slide 3
Plasmonic Amplifiers
PMMA cladding on thin nanocomposite
3/9
CdSe QDs as a probe of concept
Different cladding thicknesses (d) between 0 and 9 µm
QDs overlap mostly with SPP
Reduce losses

## Slide 4
Plasmonic Amplifiers
PMMA cladding on thin nanocomposite
4/9
Caracterization with VSL method
gain similar for all cladding thicknesses
losses reduced as long as cladding thickness is increased

## Slide 5
Plasmonic Amplifiers
PMMA cladding on thin nanocomposite
5/9
Caracterization by end fire coupling
With thick claddings it is possible to couple the pump laser from the edge (sample length~5 mm) to photonic modes in the cladding
pump excites QDs which PL can be coupled to the SPP

## Slide 6
QD Photodetectors
Photodetector with PbS QDs by LbL
6/9
Caracterization by in-house set-ups
Resistivity of the layers: r  2.105 W cm
Responsivities >1 mA/W in the visible and 0.2 mA/W at 1100 nm (exciton ground state absorption)
Photoconductive gain >10 mA/W (1 V) with whole spectrum of the lamp
- Good stability after several weeks in air

## Slide 7
Milestones
Demonstration of conductive QD layers with photoconductive properties
Demonstration of metal-(lithographic) polymer and QD metal-(lithographic) polymer nanocomposites
7/9
MS19:
MS18:
month 15
sent
sent

## Slide 8
Milestones
Demonstration and decision on photodetector
operation: nano-gap (MIM) vs Schottky/heterostructure
8/9
MS20:
month 18
D4.1:
Designs of plasmonic amplifiers
D4.2:
Report on optical properties of QDs layers and polymer nanocomposites
In progress
ok
ok

## Slide 9
Dissemination
Abstract sent to ICTON (24-27 Cartagena Spain) about bilayer structures
Conference papers and talk to SPIE Advanced lithography (24-28 Feb, 2013 California)
  Novel patternable and conducting metal-polymer nanocomposite: a step toward advanced mutlifunctional materials
  Metal-polymer nanocomposite resists: a step toward in situ nanopatterns metallization
Paper submitted to Journal of Display and Technology
  UV-Patterning of In Situ Synthesized Conducting Polymers for Polymeric Display Devices
9/9