## Slide 1
Unit of Materials and Optoelectronic Devices
University of Valencia
www.uv.es/umdo

## Slide 2
Summary
2/12
1-Amplifier
2- Photodetector
3- Milestones
4- Dissemination

## Slide 3
Plasmonic Amplifiers
PMMA cladding on thin nanocomposite
3/12
Maximize overlap SPP with QDs
Reduce losses
Possible coupling through the edge for low enough lengths and thick enough claddings
1- Pump coupled to the dielectric (TE and TM)
2- PL collected in the gold (TM)
Green beam (533 nm)
PL coupled to the SPP
Last presentation…

## Slide 4
Plasmonic Amplifiers
PMMA cladding on thin nanocomposite
4/12
Simulation of waveguides at 1.55 mm
d1≈1-1.4 µm  close to evanescent queue +avoid high order TM modes
d2 dependent on the structure.
  asymmetric: plasmonic for d2 <3 µm but for thicker claddings fundamental mode centered on the dielectric.
  symmetric: allways plasmonic

## Slide 5
Plasmonic Amplifiers
PMMA cladding on thin nanocomposite
5/12
Experimental results: samples
PbS QDs form UGENT (1.55 µm)
not high filling factor (to avoid losses)
d1 = 1 µm
d1 = [0-9] µm

## Slide 6
Plasmonic Amplifiers
PMMA cladding on thin nanocomposite
6/12
Experimental results: variable stripe method
PL coupled
gain close to zero
losses decrease with thickness of the cladding and higher in TM

## Slide 7
Plasmonic Amplifiers
PMMA cladding on thin nanocomposite
7/12
Experimental results: end fire coupling
Absorption of PbS limits strongly the pump in the visible optimize thickness and concentrations and reduce waveguide length (< 1 mm)
TE
TM

## Slide 8
QD Photodetectors
Photodetector with PbS QDs by LbL
8/12
New data by using PbS with more passivated surface
Resistivity of the layers: r  5-8.104 W cm
Responsivities 0.5 A/W in the visible and 1 mA/W at 1000 nm (exciton ground state absorption)
Photoconductive gain 50 mA/W (1 V) at single wavelength (600 nm)
Absorption edge
ITO
PDOT
QD-layer (300 nm)
Ag
TOP
S = 1 mm2
I

## Slide 9
QD Photodetectors
Photodetector with PbS QDs by LbL
9/12
New data by using PbS with more passivated surface
Resistivity of the layers: r  5-8.104 W cm
Responsivities 0.5 A/W in the visible and 1 mA/W at 1000 nm (exciton ground state absorption)
Photoconductive gain 50 mA/W (1 V) at single wavelength (600 nm)
GLASS
QD-layer (300 nm)
Ag
TOP
100 mm
I
I

## Slide 10
QD LED (600 nm)
QD-LED with CdSe/ZnS (600 nm)
10/12

## Slide 11
Milestones/Deliverables
Demonstration and decision on photodetector
operation: nano-gap (MIM) vs Schottky/heterostructure
11/12
MS20:
month 18
D4.1:
Designs of plasmonic amplifiers
D4.2:
Report on optical properties of QDs layers and polymer nanocomposites
In progress
ok
ok

## Slide 12
Dissemination
Abstract sent to ICTON (24-27 Cartagena Spain) about bilayer structures
Conference papers and talk to SPIE Advanced lithography (24-28 Feb, 2013 California)
  Novel patternable and conducting metal-polymer nanocomposite: a step toward advanced mutlifunctional materials
  Metal-polymer nanocomposite resists: a step toward in situ nanopatterns metallization
Paper submitted to Journal of Display and Technology
  UV-Patterning of In Situ Synthesized Conducting Polymers for Polymeric Display Devices
12/12