## Slide 1
Unit of Materials and Optoelectronic Devices
University of Valencia
www.uv.es/umdo
I. Suárez, P.J. Rodríguez-Cantó and J.P. Martínez-Pastor
Current State of the work
Phone Conference December 2th 2013

## Slide 2
Outline
1-Deliverables and milestones
2-Current Status of the work
2.1-Plasmonic amplifiers by using polymers doped with QDs
2.2-Photodetectors based on QDs and polymers
3- Next steps
2/8

## Slide 3
Deliverables and Milestones
 | Names of the Milestones | Month | Partner
MS16 | Decision on optimized structures for plasmonic amplifiers | 12 | UVEG
MS17 | Synthesis of nanoparticles with gain at 1550nm | 12 | UGENT
MS18 | Demonstration of conductive QD layers with photoconductive properties | 15 | UVEG
MS19 | Demonstration of metal-(lithographic) polymer and QD metal-(lithographic) polymer nanocompo-sites | 15 | UVEG
MS20 | Demonstration and decision on photodetector operation: nano-gap (MIM) vs. Schottky / heterostructure | 18 | UVEG
MS22 | Demonstration of plasmonic amplifiers with optical pumping exhibiting 10 dB gain | 21 | IMEC
MS23 | Operation of QD based photodetector with responsivity > 0.1 A/W | 24 | UVEG
MS24 | Demonstration of SPP amplifiers with electrical injection exhibiting 10dB/cm gain | 30 | UVEG
3/8

## Slide 4
Deliverables and Milestones
 | Names of the Deliverables | Month | Partner
D4.1 | Designs of plasmonic amplifiers | 18 | UVEG
D4.2 | Report on optical properties of QDs layers and polymer nanocomposites | 18 | UVEG
D4.3 | Designs of plasmonic photodetectors | 24 | UVEG
D4.4 | Report on SPP amplifiers by using QDs | 30 | IMEC
D4.5 | Report on plasmonic photodetectors | 33 | UVEG
D.7.1 | First report on NAVOLCHI dissemination and promotion activities | 18 | AIT
D.7.2 | First report on NAVOLCHI exploitation activities | 18 | AIT
4/8

## Slide 5
Plasmonics amplifiers
HgTe QDs in planar dielectric waveguides
5/8
Filling factor (ff) implies a trade-off between absorption losses and generated photoluminescence (PL)
Pump from the surface to provide a uniform excitation:
ff ≈ 0.075
g0~250 cm-1
α~80 cm-1
Aggregates or excited states?

## Slide 6
Plasmonics amplifiers
Active HgTe waveguides
6/8
This configuration can solve this trade-off by finding optimal thicknesses
g0~300 cm-1
α~20 cm-1
Aggregates or excited states?

## Slide 7
Plasmonics amplifiers
Plasmonic waveguides
7/8
Au stripes (~10 μm) by UV lift-off process
Covered by active material
Simulation of LR-SPP mode
Optical characterization (CdSe)
PMMA
PMMA
Au
Au

## Slide 8
Next steps
What’s next?
8/8
Characterization of HgTe waveguides under pulsed excitation
HgTe in Plasmonic waveguides
stripe plasmonic waveguides
- IR
- < 1 μm (e-beam)