## Slide 1: Navolchi update
Telco 3 March 2014

## Slide 2: WP4
Amplifiers:
  Work on hold till confirmation on QDot materials in film
  Gain measurements planned for later this month @TUDelft
  Fabricated SiN-waveguides for realizing optical pumped devices
MS22 submitted

## Slide 3: WP5 - Couplers
SOI devices for plasmonic couplers sent to KIT (today)
  Full wafer (diced)
Work on grating couplers started again.
  Investigating possibility for increasing coupling distance between two chips through the introduction of high index interlayer (e.g. silicon) -> less diffraction
  MS33 delayed till end April
Ge-detectors
  Question: what is next step ?
D5.3 (first gen passive devices) completed and submitted