## Slide 1
SiN-QDs microdisk vertically coupled with on-chip waveguide
Fabrication of SiN microdisks with CdSe/CdS QDs embedded
R=3.5μm
R=5.0μm
R=7.5μm
R=10μm
microscopy images of different radius disks

## Slide 2
PL characterization
Configuration of PL measurement
1. Pump with 400nm femtosecond laser on the top of disk (80MHz repetition rate, focused spot size ~ 100um diameter, ~200mW average power)
2. Collect the PL from the cleaved facet of on-chip bus waveguide using microlensed fiber
SiN disk
SiN bus waveguide
a-Si pillar
SiO2 box
Cross-sectional schematics of PL measurement
PL collect
Pump

## Slide 3
Measurement results
Normalized PL of SiN-QDs microdisks with different radius
Q=1160
Q=3406
Q=4430
Q=5749
For smaller disks, only 1st TE mode family is coupled out. For larger one, both 1st and 2nd TE mode families can be coupled out. The measurement is also limited by the resolution of monochromator for high Q modes. Further analysis is still needed…